BLANKET SPECIFICATIONS:

[image: image1.emf]Virity 

no

Ends/

cm

Picks/

cm

Weight 

gm/sqm

Weight/B

lanked in 

(Kg)

Width 

in cm

Length 

in cm

Wool & others

Warp wayWeft way

3 9 7 630 2.35 81.65 54.43 163 239 30-40% wool +

60-70% Naylkon, 

Polyester, Polynosic, 

Rayon, Acrylic & Cotton 

fiber

Toler

ance

5% 5% ±10gm 2% 2% 5% 5% 5%

Breaking Load in Kg.  

15x20 cm strip

WEIGHT : 630 Gm/Sqm
Width : 163 Cm

Length : 239 Cm
Sheet1

		Virity no		Ends/cm		Picks/cm		Weight gm/sqm		Weight/Blanked in (Kg)		Breaking Load in Kg.  15x20 cm strip				Width in cm		Length in cm		Wool & others

												Warp way		Weft way



		3		9		7		630		2.35		81.65		54.43		163		239		30-40% wool +

																				60-70% Naylkon, Polyester, Polynosic, Rayon, Acrylic & Cotton fiber

		Tolerance		5%		5%		±10gm		2%		2%				5%		5%		5%





Sheet2






