Technology Qualification & Requirement

1   specification for Cement Packing bags：

| content; Sack features. Filled sack weight (kg); 50. Material packed; PORTLAND CEMENT. A Length (mm); 615±0.5. B Width (mm); 495±0.5. C Patch height (mm); 110±0.2. D Patch length(mm); 385±0.5. E Valve depth (mm); 170±0.2. F Valve height(mm); 115±0.2. Valve Colour; Red. Valve orientation; Back left. Micro perforation:; Yes. Air Permeability; > 120 cu. M/50 mbar. Coating; 25 GSM ± 3 GSM. Bag strength; > 650 Newton in Warp direction. Bag weight; 83 GSM±2GSM. 2、Detailed design of Packing bag： |  |
| --- | --- |

The final design and specification shall be in accordance with the client’s requirement.

3, Technical requirements

Product name: two-layer plastic woven bags

Color: It shall be made according to the design, format and color provided by the client

Format requirement: it shall be made in line with the requirements provided by the client, the mark shall be clear, correct and right color

- ≤100℃. The acceptable temperature: ≤100℃

- Damage rate shall be less than 3‰, bags damaged over that rate shall be provided by the contractor free of charge.

- Package type shall be 100 pcs/bundle, easy to pack, the package fee shall be included in the quotation.

- 1±0.02m Selecting 5 sample bags arbitrarily,  these bags shall not break for over 8 times falling tests from 1±0.02m of height under the condition of ≤100℃ thermal treatment and loading 50±0.2kg sand.

- meet the national quality standards of Zambia.