

	
	
	

	
	
	

	
	
	



1 Material/材料


 H90 Brass, Hardness: 70~90HV, with Ni/Ag plating/ H90黄铜，硬度：70~90维氏,  电镀 

        镍/银；
2 Finish/成品

2.1 Plating Requirement/电镀规格规格

 Plating with Ni(1~2um) and Ag(0.5~1um) layer/端帽镀镍打底，厚度为1~2微米，表面镀银，厚度为0.5~1微米；
2.2 Finish requirement/端帽外观要求


   There shall not be a wide variation in the brightness within a consignment, and the variation within individual batches shall be minimal. Individual components are to be free from the following defects. Individual batches shall be minimal. Individual components are to be free from the following defects。同一批次的产品不能有较大的色差和亮度差别，同时不同批次的产品间色差和亮度差别应尽可能小。有以下缺陷的单个物料是不能接受并使用的，供应商需要在提供批量产品时尽可能减少以下的缺陷，这些有缺陷的单个物料需要退回并由供应商承担。

· Fissures and porous areas/裂缝及气孔

· Water and color stains/水渍及色斑

· Un-plated areas and dull patches/未电镀区及暗色块

· Peeling of plating/镀层脱落或起皮

· Adhesion of salts or dust/粘有盐或污浊物

· Local build up of metal/局部有多余金属物

2.3 Requirement of Solder ability
         The plating thickness should be average, the solder-ability should meet IEC60068-2-20 Method 1./镀层必须均匀一致，可焊性满足IEC60068-2-20 实验方法1
3 Technical Drawing/技术图纸
[image: image1.png]o oo secTones
! \ i
| S
} RO.10
I gt
H -0.05
|
|
i +0.02
o ow3E o
280.902

S0

#002
0207502




4 Packing and Identification/包装和标示

All packaging must be constructed so as to be of sufficient strength and quality to ensure that parts are protected from damage during transit. In addition and agreed quality of parts shall be supplied in suitably sealed polythene bags so as to exclude liquids, including water of any form, compounds containing chlorine or sulfur, dust and extraneous packing material such as particles of cardboard./ 所有的包装必须有足够的强度和质量以便在运输途中能防止被损坏。合格物料使用聚乙烯塑料袋封好以免受任何形式的水分,氯化物或硫化物,灰尘,以及其它包装材料如纸板碎屑的影响.
The following information must be clearly marked on the packaging/下列内容必须清楚地标在包装上：
· Quantity/数量

· Part Identification including Bussmann part and issue number/零件标示(包括料号和发行编号)

· Manufacturers Batch Number and Date of Manufacturer/生产批次号和生产日期
5 Certificate of Conformity/符合性声明

A CERTIFICATE OF CONFORMITY WITH THIS SPECIFICATION MUST BE SUPPLIED WITH EACH CONSIGNMENT. ADDITIONAL QUALITY DOCUMENTATION MAY BE REQUIRED IN AN AGREED FORMAT. 每一批货物均需要有关于该技术规格的符合性声明,同时相关的质量文件需要按要求的格式提供

The CoC must include the following information/符合性声明必须包括以下几个内容

· Dimension OQC report/尺寸出厂检验报告

· CoC of Raw Material/材质证明

· Plating thickness OQC report/电镀层厚度测试报告

A CERTIFICATE OF CONFORMITY WITH THIS SPECIFICATION AND RoHS DIRECTIVE (2002/95/EC) MUST BE SUPPLIED WITH EACH CONSIGNMENT. 每一批货物均需要有关于该技术规格和ROHS指令（2002/95/EC）的符合性声明
	
	
	
	
	
	

	
	
	
	
	
	



