RAW MATERIAL SPECIFICATION.,

ELECTRODE PASTE (STANDARD CYLINDER 0.45M / 0.50M DIAMETER) – 1000 MM HEIGHT

Quality :  20 – 30%

SPECIFICATON		TYPICAL

Plasticity	20 – 30 %	23%

Binder Content	21.9 – 24.4 %

Ash	3.0 – 6.0 %

Density	1537 – 1607 kg/m3

Volatiles	12 – 16 %		10%

Fixed Carbon	80 – 87		85%

Plasticity  : Classification in the groups within the area 15 -40 %

Quality (20 -30%)	Briquettes, blocks & 200,400 & 500 mm cylinder

Baked Paste at 1000 ⁰ C

Apparent density	1360 kg/m3

Electricity resistivity	68 µΩ

Electricity resistivity *)	40 µΩ

Thermal Conductivity *)	8 W/(k.m)

Specific heat*)	1.8 kj/(k.kg)

Compressive Strength	17 N/mm2

Bending Strength	3.5 N/mm2

Young’s modulus	3.5 N/mm2

Ash Content	5 %

Phosphorus	0.02 %

Sulphur	0.50 %

*) Measured at 100⁰ C, other measurements are at room temperature

Typical Characteristics

Unbaked Paste

Volatiles	10 %

Fixed Carbon	85 %

Apparent Density	1570 kg/m3

Thermal Conductivity	2.5 W/(k.m)

Specific heat	0.9 kj/(k.kg)

The above data applies to both electrode paste cylinders & briquettes which are produced with a  slightly different softening points 63⁰ C for cylinders & 80-90⁰ C for briquettes.

(measure with ‘Ring & Ball” method