|  | Casing Pipe 508x11,13(20^) API, J55,R-3, thread type BC, - P≤0.020, S≤0.010 - set of nonmetallic inclusions 12 levels, - yield strength- ≥58000 psi(400MPa), ultimate tensile strength- ≥76415 psi(527MPa), Tensile coefficient=24% Crush resistance,MPa(kg/cm2) ≥3,59 Internal pressure: Corresponding to yield strength for smooth part and for joints MPa(kg/cm2) pipe body:14.5 ; coupling:14.5 - outer diameter tolerance:-0,4%D+0,1%D Ovality: 80% of outer diameter tolerance Wall thickness tolerance: pipe body:-10%t +12%t pipe end:-10%t+15%t Variation variegated: 80% of the wall thickness tolerance Straightness: 0,15%L inner diameter:485,74mm bore diameter: 480,98mm Length limits: R-3, 10,97-11,8≥5%10,36-10,97 API 5CT Nominal weight of the pipe, including threading and coupling (kg / m): 139,89 Weight 1 m smooth part of the pipe (kg / m):36,38 - thread tolerance (inclined-stepped threads BC) sealing distance ,pipe +0,25 +2,25mm; coupling: -2,50 0,60mm Thread pitch: every inch±0,003(±0,077mm) cumulatively±0,004"(±0,102mm) tooth height: ±0,001"(0,026mm) taper tube:0,0818"-0,0868"(2,08-2,20 mm) taper coupling: 0,0808"-0,0878"(2,05-2,23mm) - flaw detection requirements ISO9303 ASTM E213 within the enterprise, the degree of control flaw detection is L3, higher than the requirements of the standard L4 - Geometrical dimensions of the threaded connection Casing pipe size:508x11.13 thread height: 1,575 mm thread pitch:5,08mm The number of threads on the length of 25.4mm-5 | 285 tonn |
| --- | --- | --- |